Hellenic Accreditation System

Annex F1/17 to the Certificate No. 663-6

SCOPE of ACCREDITATION of the Testing Laboratory of TRYPSIANIS GRIGORIOS

| Materials/ Products to be tested | Types of test/ Properties to be measured | Applied methods/ Techniques to be used |
| --- | --- | --- |
| Physical Tests |
| Hardened Concrete | Testing hardened concrete Part 2: Making and curing of test specimens (15cm x 15cm x 15cm) for strength tests | ELOT ΕΝ 12390-2: 2019 |
| Aggregates | 1.Tests for geometrical properties – Part 1: Determination of particle size distribution – Sieving method | ΕLΟΤ ΕΝ 933.01:2012 ΕLΟΤ ΕΝ 932.02:2000 |
|  | 2.Test for geometrical properties – Part 3: Determination of particle shape – Flakiness index | ΕLΟΤ ΕΝ 933.03:2012 ΕLΟΤ ΕΝ 932.02:2000 |
|  | 3.Test for geometrical properties – Part 4: Determination of particle shape – Shape index | ΕLΟΤ ΕΝ 933.04:2008 ΕLΟΤ ΕΝ 932.02:2000 |
|  | 4.Test for geometrical properties – Part 8: Assessment of fines. Sand equivalent test. | ΕLΟΤ ΕΝ 933.08:2012+A1:2015 ΕLΟΤ ΕΝ 932.02:2000 |
|  | 5.Test for mechanical and physical properties – Part 6: Determination of particle density and water absorption. | ΕLΟΤ ΕΝ 1097.06:2013 ΕLΟΤ ΕΝ 932.02:2000 |
|  | 6.Tests for thermal and weathering properties – Part 2: Magnesium sulfate test (test of rock health). | ΕLΟΤ ΕΝ 1367.02:2010 ΕLΟΤ ΕΝ 13450:2003 (Παράρτημα C) ΕLΟΤ ΕΝ 932.02:2000 |
| Bituminous mixtures | 1.Bituminous mixtures – Test methods for hot mix asphalt – Part 2: Determination of particle size distribution | ELOT ΕΝ 12697.02+Α1:2019 |
|  | 2.Bituminous mixtures – Test methods for hot mix asphalt – Part 5: Determination of the maximum density | ELOT ΕΝ 12697.05:2019 |
|  | 3.Bituminous mixtures – Test methods for hot mix asphalt – Part 6: Determination of bulk density of bituminous specimens | ELOT ΕΝ 12697.06:2020 |
| Mechanical tests |
| Aggregates | 1.Tests for mechanical and physical properties of aggregates - Part 1: Determination of the resistance to wear (micro-Deval) | ΕLΟΤ EN 1097.01:2011 |
|  | 2.Tests for mechanical and physical properties – Part 2: Methods for the determination of resistance to fragmentation (Los Angeles test) | ΕLΟΤ EN 1097.02:2020 |
| Masonry units | Determination of compressive strength | ΕLΟΤ ΕΝ 772.01:2011+A1:2015 |
| Hardened Concrete | 1.Testing hardened concrete – Part 3: Compressive strength of test specimens | ELOT ΕΝ 12390.03:2019 |
|  | 2.Testing concrete in structures - Part 1: Cored specimens - Taking, examining and testing in compression | ELOT ΕΝ 12504.01:2020 |
| Bituminous mixtures | 1.Bituminous mixtures – Test methods for hot mix asphalt – Part 30: Specimen preparation by impact compactor | ELOT EN 12697.30:2019 |
|  | 2.Bituminous mixtures – Test methods for hot mix asphalt – Part 34: Marshall test | ELOT ΕΝ 12697.34:2020 |
| Chemical Tests |
| Aggregates | Tests for geometrical properties of aggregates Part 9: Assessment of fines – Methylene blue test | ΕLΟΤ ΕΝ 933.09:2009+A1:2013 |
| Bituminous mixtures | Bituminous mixtures – Test methods for hot mix asphalt – Part 1: Soluble binder content | ELOT ΕΝ 12697.01:2020 (Annex B §B.1.5 & B.2.1) |

Site of assessment: Laboratory permanent premises, Sindos Industrial Area, Thessaloniki, Greece

Approved signatories: Gr. Tripsianis .

This Scope of Accreditation replaces the previous one dated 08.07.2022.

The Accreditation Certificate No.663-6, to ELOT EN ISO/IEC 17025:2017, is valid until 22.03.2027.

Athens, 09.04.2024

Christos Nestοras

CEO of ESYD