Hellenic Accreditation System

Annex F1/21 to the Certificate No. 134-6

| SCOPE of ACCREDITATION of the Quality Control Testing Laboratory of NDT Technology – Athanassios Gkiokas |
| --- |
| Materials / Products to be tested | Types of tests / Properties to be measured | Applied methods / Techniques to be used |
| Non-destructive tests using magnetic particles |
| Ferromagnetic materials | In situ inspection with magnetic particles and Yoke AC, HWDC & DC | EΝ ISO 10893-5: 2011 Non-destructive testing of steel tubes – Part 5: Magnetic particle inspection of seamless and welded ferromagnetic steel tubes for the detection of surface imperfections |
|  |  | ASME 2023 Boiler and Pressure Vessel Code. Section V, Non Destructive Examination. Article 7: Magnetic Particles Examination |
|  |  | EN ISO 9934-1: 2016 Non-destructive testing – Magnetic particle testing – Part 1: General principles |
|  |  | ΕΝ 1369: 2012 Founding – Magnetic particle inspection |
|  |  | EN ISO 17638: 2016 Non-destructive testing of welds – Magnetic particle testing |
|  |  | ΕΝ 10228-1: 2016 Non-destructive testing of steel forgings – Part 1: Magnetic particle inspection |
|  |  | ASTM E3024/E3024M-22a (αντικατέστησε το ASTM E 1444/ Ε 1444 Μ: 2016 e1) Standard practice for magnetic particle examination |
|  |  | ASTM E 709: 2021 Standard guide for magnetic particle examination |
| Non-destructive tests using penetrant fluids |
| Metallic materials | In situ inspection with visible and/or dye penetrants / Surface imperfections | EN ISO 10893-4: 2011 Non-destructive testing of steel tubes – Part 4: Liquid penetrant inspection of seamless and welded steel tubes for the detection of surface imperfections |
|  |  | ΕΝ 10228-2: 2016 Non-destructive testing of steel forgings – Part 2: Penetrant testing |
|  |  | ΕΝ 1371-1: 2011 Founding – Liquid penetrant inspection – Part 1: Sand, gravity die and low pressure die castings |
|  |  | ASTM E 165: /E165M: 2023 Standard test method for liquid penetrant examination |
|  |  | ASME 2023 Boiler and Pressure Vessel Code. Section V, Non Destructive Examination. Article 6: Liquid Penetrant Examination |
|  |  | EN ISO 3452-1: 2021 Non-destructive testing – Penetrant testing – Part 1: General principles |
|  |  | ASTM E 1417/ Ε 1417 Μ-21e1 Standard practice for liquid penetrant examination |
| Non-destructive tests using the Eddy current method |
| Conductive, non-ferromagnetic tubular products | Eddy Current Testing / Surface and/or subsurface and/or internal discontinuities Eddy Current Testing / Surface and/or subsurface and/or internal discontinuities (cont.) | ASTM E 243: 2018 Standard Practice for Electromagnetic (Eddy-Current) Examination of Copper and Copper-Alloy Tubes |
|  |  | ASME 2023 Boiler and Pressure Vessel Code. Section V, Non Destructive Examination. Article 8 : Eddy Current Examination of tubular products |
| Seamless and welded tubular products, austenitic stainless steel and similar alloys |  | ASTM E 426 -16 (2021) Standard Practice for Electromagnetic (Eddy-Current) Examination of Seamless and Welded Tubular Products, Austenitic Stainless Steel and Similar Alloys |
| Welds of electrical conductive materials |  | EN ISO 17643:2015 Non-destructive examination of welds – Eddy current examination of welds by complex plane analysis |
| Non-magnetic heat exchanger tubes |  | ASTM E 690-15(2020) Standard Practice for In Situ Electromagnetic (Eddy-Current) Examination of Nonmagnetic Heat Exchanger Tubes |
| Non-destructive test – Measurement of surface hardness |
| Materials and welds of steel, cast steel and cast iron | In situ measurement of surface hardness | ASTM A 956/A956M-22 Standard Test Method for Leeb Hardness Testing of Steel Products |
| Non-destructive tests – Coating thickness measurements |
| Non-magnetic base metallic materials | Thickness measurements of non-conductive coatings with the Eddy Current method (0-1600μm) | ISO 2360: 2017 Non-conductive coatings on non-magnetic basis metals – Measurement of coating thickness – Eddy current method |
| Magnetic base metallic materials | Thickness measurements of non-magnetic coatings with the magnetic method (0-1600μm) | ASTM B499-09(2021)e1 Standard Test Method for Measurement of Coating Thickness by the Magnetic Method: Nonmagnetic Coatings on Magnetic Basis Metals |
| Ultrasonic non-destructive tests |
| Metallic materials and welds | Ultrasonic testing / Internal discontinuities Ultrasonic testing / Internal discontinuities (cont.) | ASME 2023 Boiler and Pressure Vessel Code. Section V, Non Destructive Examination. Article 4: Ultrasonic Examination Methods for In-service Inspection |
|  |  | ASME 2023 Boiler and Pressure Vessel Code. Section V, Non Destructive Examination. Article 5: Ultrasonic Examination Methods for Materials and Fabrications |
| Welds of metallic materials |  | EN ISO 17640: 2018 Non destructive testing of welds – Ultrasonic testing – Techniques, testing levels and assessment |
| Flat steel products |  | ΕΝ 10160: 1999 Ultrasonic testing of steel flat product of thickness equal or greater than 6 mm (reflection method) |
| Ferritic and martensitic steel forgings |  | ΕΝ 10228-3: 2016 Non-destructive testing of steel forgings – Part 3: Ultrasonic testing of ferritic or martensitic steel forgings |
| Industrial products that permit the transmission of ultrasound |  | EN ISO 16810:2014 Non-destructive testing – Ultrasonic examination – Part 1: General principles |
| Steel forgings |  | ASTM A 388/A 388M: 2019 Recommended practice for ultrasonic testing and inspection of heavy steel forgings |
| Steel castings |  | ASTM A609 / Α609Μ-12(2023) Standard specification for longitudinal beam ultrasonic inspection of carbon and low-alloy steel castings |
| Steel plates |  | ASTM A435 / A435M: 17 (2023) Standard specification for straight-beam ultrasonic examination of steel plates |
| Any material in which ultrasonic waves can propagate | Ultrasonic thickness testing | ASTM E 797/ E797M-21 Standard Practice for Measuring Thickness by Manual Ultrasonic Pulse-Echo Contact Method |

Site of assessment: Permanent laboratory premises, Levedou 2-4 & Andrea Dimitriou, 16121 Kesariani, Attiki, Greece.

Approved signatory: A. Gkiokas.

This Scope of Accreditation replaces the previous one dated July 23rd , 2023.

The Accreditation Certificate No. 134-6, to ELOT EN ISO/IEC 17025: 2017, is valid until 23.7.2028.

Athens, February 2nd, 2024

Christos Nestoras

CEO of ESYD