Hellenic Accreditation System

Annex F1/11 to the Certificate No. 494-6 SCOPE of ACCREDITATION of the Standard Chemical Laboratory of Southern Greece of the SECTION SES MEGALOPOLIS of the PPC S.A.

| Tested materials and products | Types of test/ Properties to be measured | Applied standards/ Techniques to be used |
| --- | --- | --- |
| Chemical testing |
| Solid mineral fuel | Determination of moisture | ASTM D 7582-15 |
|  | determination of total carbon,hydrogen,nitrogen and sulphur | In house method (EASF) based on ISO 29541:2010 ISO 15178:2000 |
|  | determination of gross and net calorific value | ISO 1928:2020 |
|  | determination of proximate analysis | ASTM D 7582-15 |
|  | determination of residual fuel in ash sample (bottom or fly) | ASTM D 7582-15 |
| limestone aggregates | Determination of moisture content by drying | ASTM C 566-19 |
| limestone aggregates | determination of carbon dioxide | ΕLΟΤ ΕΝ 12485:2017 |

| Tested materials and products | Types of test/ Properties to be measured | Applied standards/ Techniques to be used |
| --- | --- | --- |
| Liquid fuels | 1.determination of water content | ASTM D 6304-20 |
|  | 2.determination of total carbon, hydrogen, nitrogen and sulphur | ASTM D 529-21 ASTM D 5623-19 |
|  | 3.determination of gross and net calorific value | ASTM D 4809-2018 |

Site of assessment: Laboratory Permanent Premises, Megalopoli SES, UNIT IV, Arcadia, Greece

Approved signatories: M.Kontou

This Scope of Accreditation replaces the previous one dated 30.07.2021.

The Accreditation Certificate No. 494-6, to ELOT EN ISO/IEC 17025:2017, is valid until 07.01.2025.

Athens, 22.11.2022

Christos Nestoras

CEO of ESYD