Hellenic Accreditation System

Annex F1/4 to the Certificate No. 1231 SCOPE of ACCREDITATION of the Testing Laboratory of the G. GKRINTZOS CIVIL WORKS CONSULTANTS IKE G. GKRINTZOS CWC

| Materials/Products tested | Types of test/Properties measured | Applied methods/Techniques used |
| --- | --- | --- |
| Physical & Chemical Tests |
| Hardened concrete | 1. Testing hardened concrete - Part 2: Making and curing specimens (15cm x 15cm x 15cm) for strength tests | ELOT ΕΝ 12390-2:2019 |
| Freshly mixed Concrete | 1. Testing fresh concrete – Part 2: Slump test | ELOT ΕΝ 12350-2:2019 |
|  | 2. Testing fresh concrete – Part 7: Air content – Pressure Methods | ELOT ΕΝ 12350-7:2019, § 6 |
| Aggregates | 1. Tests for geometrical properties of aggregates – Part 1: Determination of particle size distribution – Sieving Method | ELOT ΕΝ 933-1:2012 |
|  | 2. Tests for geometrical properties of aggregates – Part 8: Assessment of fines – Sand equivalent test | ELOT ΕΝ 933-8:2012 + A1:2015 |
| Soils | 1. Standard Test Method for Density and Unit Weight of Soil in Place by Sand-Cone Method | ASTM D1556/D1556M-15e1 |
|  | 2. Standard Test Methods for In-Place Density and Water Content of Soil and Soil-Aggregate by Nuclear Methods (Shallow Depth) | ASTM D6938-2023 |
| Bituminous mixtures | 1. Bituminous mixtures - Test methods - Part 1: Soluble binder content | ELOT ΕΝ 12697-1:2020 |
|  | 2. Bituminous mixtures - Test methods - Part 2: Determination of particle size distribution | ELOT ΕΝ 12697-2:2015 +Α1:2019 |
|  | 3. Bituminous mixtures - Test methods - Part 5: Determination of the maximum density | ELOT ΕΝ 12697-5:2019 |
|  | 4. Bituminous mixtures - Test methods - Part 6: Determination of bulk density of bituminous specimens | ELOT ΕΝ 12697-6:2020 |
| Mechanical Tests |
| Hardened concrete | 1. Testing concrete in structures – Part 1: Cored specimens – Taking, examining, and testing in compression | ELOT ΕΝ 12504-1:2020 |
|  | 2. Testing hardened concrete – Part 3: Compressive strength of test specimens | ELOT ΕΝ 12390-3:2019 |
| Aggregates | 1. Tests for mechanical and physical properties of aggregates - Part 2: Methods for the determination of resistance to fragmentation, Los Angeles test | ELOT ΕΝ 1097-2:2020 |
| Bituminous mixtures | 1. Bituminous mixtures - Test methods - Part 30: Specimen preparation by impact compactor | ELOT ΕΝ 12697-30:2019 |
|  | 2. Bituminous mixtures - Test methods - Part 34: Marshall test | ELOT ΕΝ 12697-34:2020 |
|  | 3. Road marking materials-Road marking performance for road users and test methods | ELOT ΕΝ 1436:2018 |
|  | 4. Road and airfield surface characteristics - Test methods - Part 4: Method for measurement of slip/skid resistance of a surface: The pendulum test | ELOT ΕΝ 13036-4:2011 |

Site of assessment: Permanent Premises, Dim. Chr. Beka 150 & Dimosthenous st., 19004 Spata, Attiki.

Approved signatory: G. Gkrintzos, S. Syrros, K. Giannoukos.

This scope of Accreditation replaces the previous one, dated 16.03.2023.

The Accreditation Certificate No.1231 to ELOT EN ISO/IEC 17025:2017, is valid until 13.01.2025.

Athens, 20.02.2024

Christos Nestoras

CEO of ESYD