Hellenic Accreditation System

Annex F1/12 to the Certificate No.02-6

| SCOPE of ACCREDITATION of the Solar & other Energy Systems Testing Laboratory of the NCSR ‘‘DEMOKRITOS’’ |
| --- |
| Tested material/ products | Types of tests/ Properties measured | Applied Standards |
| Glazed liquid heating solar collectors | Steady–state outdoor tests: Thermal output Effective thermal capacity Time constant Incidence angle modifiers Pressure drop Internal pressure High temperature resistance Stagnation temperature Exposure External thermal shock Internal thermal shock Rain penetration Impact resistance Mechanical load | ISO 9806:2017 |
| Domestic solar water heating systems | Tests for system performance characterization and yearly performance prediction Over temperature protection Pressure resistance | ELOT EN 12976-2:2019 ISO 9459-2:1995 ISO 9459-5:2007 |

Site of assessment: Permanent laboratory premises, Aghia Paraskevi, Attiki

Approved signatory: Stamatis Babalis, E. Mathioulakis

This Scope of Accreditation replaces the previous one dated 10.12.2020.                                                                The Accreditation Certificate No. 02-6, to ELOT EN ISO/IEC 17025:2017, is valid until 17.06.2024.

Athens, 28.11.2022

Christos Nestoras

CEO of ESYD

# Text boxes

Performance tests