Hellenic Accreditation System

Annex F1/16 to the Certificate No. 113-5

SCOPE of ACCREDITATION of the Laboratory Testing Center of the Corinth Pipeworks S.A.

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
| Mechanical tests |
| Metallic Materials | 1. Tensile Test on Metallic Materials / Tensile Strength (N/mm²), Yield Point (N/mm²), Elongation (%) | ASTM E8/E8M-21 ISO 6892-1: 2019 (0-1200)kN |
|  | 2. Impact (Charpy) Test / Impact resistance (J) | ASTM E23-18 ISO 148-1: 2016 (0-750)J |
|  | 3. Bend Test | ISO 5173: 2009+A1:2011 (0-180)° |
|  | 4. Vickers Hardness / Hardness (HV) | ISO 6507-1: 2018 HV10 (450HV10 max) |
| Chemical tests |
| Carbon and low-alloy steel | Analysis with atomic emission spectrometry | ASTM E415-17 |

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |

| Non-destructive tests |
| --- |
| Steel strip/plate used for the manufacture of welded steel tubes | 1. Ultrasonic Test (Thickness 6,4 – 40mm) | EN ISO 10893-9: 2011 & A1:2020 ASTM A435/A435M-17 |
| Weld of welded steel tubes |  | EN ISO 17640: 2018 EN ISO 10893-8: 2011 & A1:2020 EN ISO 10893-11: 2011 & A1:2020 ASTM E273-20 ASTM E587-15 (2020) |
| Weld of welded steel tubes | 2. Radiographic inspection using X-rays (Penetration thickness ≤40mm) | EN ISO 17636-1: 2013 EN ISO 17636-2: 2013 EN ISO 10893-6: 2019 EN ISO 10893-7: 2019 ASTM E94/E94M-17 |

Site of assessment:  Permanent laboratory premises, Thisvi Plant, Viotia, Greece.

Approved signatories: Tazedakis Ath., Armakolas Ι., Stathi Ι., Tasios L. (Mechanical/Chemical Tests), Tazedakis Ath., Voudouris N., Tsakoumas Th., (Non-destructive Tests)

This Scope of Accreditation replaces the previous one dated August 27th, 2020.

The Accreditation Certificate No. 113-5, to ELOT EN ISO/IEC 17025: 2017, is valid until 9.1.2023.

Athens, January 19th, 2022

Christos Nestoras

CEO of ESYD