Hellenic Accreditation System

Annex F1/19 to the Certificate No. 23-7

SCOPE of ACCREDITATION of the Testing Laboratory of Group Research, Innovation and Quality Department of TITAN Cement Company S.A.

| Tested materials/ Products | Types of test/ Properties to be measured | Applied standards/Techniques to be used |
| --- | --- | --- |
| Chemical tests |
| Coal | Determination of total moisture | ISO 589:2008 Method A2 |
| Coke | Moisture determination | ISO 687:2010 |
| Coal/Coke | Determination of total sulfur | ISO 334:2020 |
| Solid mineral fuels | 1.Determination of ash content | ISO 1171:2010 |
|  | 2.Determination of total carbon, hydrogen and nitrogen | ISO 29541:2010 |
|  | 3.Determination of gross calorific value and calculation of net calorific value | ISO 1928:2020 |
| Raw meal | 1.CO2 determination | In house method based on ELOT ΕΝ 196-2 :2013 §4 (Μ43) |
|  |  | In house method with the use of Differential Scanning calorimetry – Thermogravimetry (Μ45) |
|  | 2.Determination of major elements | In house method based on ELOT ΕΝ 196-2:2013 §4 (Μ44) |
|  | 3.Determination of total organic carbon (TOC) | In house method based on ELOT ΕΝ 13639:2017 §6 (Μ46) |
| Cement Cement (continued) | 1.Determination of major elements | ELOT ΕΝ 196-2:2013 §4 |
|  | 2.Determination of the water –soluble chromium(VI) | ELOT ΕΝ 196-10:2016 |
|  | 3.Determination of total organic carbon (TOC) | In house method based on ELOT ΕΝ 13639:2017 §8 (Μ46) |
| Limestone | Determination of total organic carbon (TOC) | ELOT ΕΝ 13639:2017 |
| Clinker | 3.Determination of total organic carbon (TOC) | In house method based on ELOT ΕΝ 13639:2017 §8 (Μ46) |

Site of assessment:     Permanent laboratory premises, Kamari Plant, Elefsis

Approved signatories: Marios Katsiotis, Dimitrios Papageorgiou.

This Scope of Accreditation replaces the previous one dated 01.06.2023.

The Accreditation Certificate No. 23-7, to ELOT EN ISO/IEC 17025:2017, is valid until 04.07.2025.

Athens, 09.10.2023

Christos Nestoras

CEO of ESYD