Hellenic Accreditation System

| Annex F1/20 to the Certificate No. 65-7 SCOPE of ACCREDITATION of the Analytical Testing Laboratories of SPECTRUMLABS S.A. |
| --- |
| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| 1. Petroleum products | Determination of sulfur content by EDXRF (% mass) | ASTM D4294-21 ISO 8754: 2003 (2021) |
|  | Determination of kinematic viscosity and calculation of dynamic viscosity (mm2/s, cSt) | ASTM D445-21e1 ISO 3104: 2020 |
|  | Determination of total sediment by hot filtration, TSE (% mass) | ISO 10307-1:2009 (2019) ASTM D 4870-18 |
|  | Determination of total sediment by thermal ageing, TSP (Procedure A) and chemical ageing, TSA (Procedure B) (% mass) | ISO 10307-2:2009 (2019) IP 390: 2011 (2017) ASTM D 4870-18 |
|  | Determination of flash point (0C) | ASTM D93-20 ISO 2719: 2016 & Amd1: 2021 |
|  | Determination of CCAI (Calculated Carbon Aromaticity Index) for petroleum products | ISO 8217: 2017 Annex F |
|  | Determination of Density by Digital Density Meter - Oscillating U-tube method | ASTM D4052-18a ISO 12185: 1996 |
|  | Determination of water content by distillation (% mass) | ASTM D95-13 (2018) ISO 3733: 1999 (2021) |
|  | Determination of pour point (0C) | ASTM D97-17b ISO 3016: 2019 |
|  | Determination of Al, Si, V, Ni, Fe, Na, Ca, Zn in residual fuel oil (mg/kg) | IP 501: 2005 (2019) |
| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| 1. Petroleum products | Determination of ash (% mass) | ISO 6245: 2001 (2018) ASTM D482-19 |
|  | Determination of cold filter plugging point (CFPP) (0C) | EN 116: 2015 ASTM D 6371-17a IP 309: 2016 |
|  | Determination of hydrogen sulfide in liquid phase (H2S) (mg/kg) | IP 570:2015 Procedure A ASTM D7621-16 (2021) |
|  | Determination of carbon residue – method (MCR) (% m/m) | ASTM D4530-15 (2020) ISO 10370: 2014 |
| 2a. Low-alloy steel | Determination of C, Si, Mn, P, S, Cr, Ni, Mo, Cu | ASTM E415-21 |
| 2b. Aluminum and aluminum alloys | Determination of Cd, Cr, Cu, Fe, Mg, Mn, Ni, Pb, Si, Sn, Zn, Ti, V | ASTM E1251-17a |
| 2c. Copper and copper alloys | Determination of Al, As, Co, Cr, Fe, Mn, Ni, P, Pb, S, Sb, Si, Sn, Zn, Ag, Bi | ΕΝ 15079: 2015 |
| 3. Water (drinking, surface, wastewater) | Determination of pH | ISO 10523: 2008 (2017) |
|  | Determination of conductivity (μS/cm) | ISO 7888: 1985 (2017) |
|  | Determination of nitrate (mg/L) | In house method Q.P. 4.9.8-ΟΕ3 |
|  | Determination of turbidity (NTU) | ISO 7027-1: 2016 (2021) |
|  | Determination of total suspended solids (TSS) (mg/L) | APHA SM 2540D |
|  | Determination of total residual oxidant (TRO) (mg/L) | ISO 7393-2:2017 |
| Welds, metallic materia | Tensile test (Proof Strength not included) | ΕΝ ISO 6892-1: 2019 ΕΝ ΙSO 15614-1: 2017 & A1: 2019 EN ISO 4136: 2022 ASTM E8/E8M-21 ΕΛΟΤ 1421-3: 2007 EN 10080: 2005 ΕΝ ISO 15630-1: 2019 ASME IX: 2021 / QW 150 EN ISO 5178: 2019 |
|  | Hardness test according to the Vickers method | ΕΝ ISO 6507-1: 2018 (HV-10, HV-30) EN ISO 9015-1: 2011 ASTM E92-17 |
|  | Bend test | EN ISO 5173: 2010 & A1: 2011 EN ISO 7438: 2020 ΕΛΟΤ 934: 1988 ASTM E290-14 ASME IX: 2021 / QW 160 ΕΛΟΤ 1421-3: 2007 EN 10080: 2006 EN ISO 15630-1: 2019 |
| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| Welds, metallic materials (con.) | Impact test according to the Charpy method | EN ISO 9016: 2022 ΕΝ ISO 148-1: 2016 ASME IX: 2021 / QW 170 |
| Welds, metallic and cast materials | Macroscopic and microscopic examination | EN ISO 17639: 2022 EN ISO 6520-1:2007 ASTM E1351-01 (2020) ASME IX:2021 / QW 183 ΕΝ ISO 15614-2:2005 |
| Reinforced plastic composites | Determination of tensile properties | ΕΝ ISO 527-1: 2019 ΕΝ ISO 527-4: 2021 |
| Materials and articles in contact with foodstuffs — Plastics | Determination of flexural properties | ΕΝ ISO 14125: 1998 & A1: 2011 EN ISO 178: 2019 |
|  | Determination of the textile glass and mineral fillet content | ΕΝ ISO 1172: 1999 |
|  | Overall migration of substances in food simulants (aqueous, ethanol 95%, isooctane) by total immersion or article filling | EN 1186-1: 2002 EN 1186-3: 2002 EN 1186-9: 2002 EN 1186-14: 2002 |

Site of assessment:   Laboratory permanent premises, Efplias 49, Piraeus, Greece.

Approved Signatories: N. Hatzopoulos, E. Mante, K. Βerketis, M. Koukouli.

This Scope of Accreditation replaces the previous one dated February 7th, 2022.

The Accreditation Certificate No. 65-7, to ELOT EN ISO/IEC 17025: 2017, is valid until 28.02.2026.

Athens, August 2nd, 2022

Christos Nestoras

CEO of ESYD

# Text boxes

###### Chemical tests

###### Mechanical tests