Hellenic Accreditation System

Annex F1/13 to the Certificate No. 796-3

SCOPE of ACCREDITATION of the Testing Laboratory of “BITULAB Ltd”

| Materials/ Products to be tested | Types of test/ Properties to be measured | Applied Standards/ Techniques to be used |
| --- | --- | --- |
| Mechanical tests |
| Hardened Concrete | Testing hardened concrete – Part 3: Compressive strength of test specimens(15cm x 15cm x 15cm) | ELOT EN 12390.03:2019 |
| Bituminous Mixtures | 1.Bituminous mixtures - Test methods – Part 34: Marshall test | ΕΝ 12697-34:2020 |
|  | 2.Test methods for hot mix asphalt – Part 12: Determination of the water sensitivity of bituminous specimen | ΕΝ 12697-12:2018 (Method A) |
|  | 3.Test methods– Part 23: Determination of indirect tensile strength of bituminous specimen | ΕΝ 12697-23:2017 (Specimen with diameter 100±3 mm) |
|  | 4.Test methods for hot mix asphalt – Part 30: Specimen preparation by impact compactor | ΕΝ 12697-30:2018 |
| Physical tests |
| Aggregates | 1.Tests for geometrical properties of aggregates - Part 1: Determination of particle size distribution - Sieving method | EN 933-1:2012 |
|  | 2.Tests for geometrical properties of aggregates - Part 8: Assessment of fines - Sand equivalent test | ΕΝ 933-8: 2012+A1:2015 |
|  | 3.Unbound and hydraulically bound mixtures – Part 2: Test methods for laboratory reference density and water content – Proctor compaction | EN 13286-2:2010/AC:2012 |
| Aggregates and Soils | 1.Determination of on-site soil density by the method of sand and the help of the cone | National Specification Ε106:1986, Test 2 |
|  | 2.Standard method for liquid limit | National Specification Ε105:1986, Test 5 |
|  | 3.Standard method for plastic limit and plasticity index | National Specification Ε105: 1986, Test 6 |
| Bituminous Mixtures | 1.Test methods – Part 2: Determination of particle size distribution | ΕΝ 12697-2:2015+A1:2019 |
|  | 2.Test methods for hot mix asphalt – Part 5: Determination of maximum density | ΕΝ 12697-5:2018 Procedure A: Volumetric Procedure |
|  | 3.Bituminous mixtures - Test methods – Part 6: Determination of bulk density of bituminous specimens | EN 12697-6:2020 |
|  | 4.Bituminous mixtures - Test methods - Part 8: Determination of void characteristics of bituminous specimens | ΕΝ 12697-8:2018 |
|  | 5.Test methods for hot mix asphalt – Part 28: Preparation of samples for determining binder content, water content and grading | ΕΝ 12697-28:2020 |
|  | 6.Bituminous mixtures - Test methods – Part 29: Determination of the dimensions of a bituminous specimen | ΕΝ 12697-29:2020 |
| Bituminous Mixtures | Test methods for hot mix asphalt – Part 1: Soluble Binder Content (Centrifuge extractor method) | ΕΝ 12697-1:2012 (ANNEX B § B.1.5 & § B.2.1) |
| Sampling |
| Bituminous Mixtures | Test methods – Part 27: Sampling | ΕΝ 12697-27:2017 § 4.3 - 4.8 |

Site of assessment:  Permanent premises, Aravissos, 58100, Giannitsa, Greece

Approved signatory: Ch. Triantafillidis

This Scope of Accreditation replaces the previous one dated   03.11.2021.

The validation of the Accreditation Certificate No. 796-3 to ELOT EN ISO/IEC 17025:2017 is extended until 18.06.2024.

Athens, 15.03.2024

Christos Nestoras

CEO of ESYD

# Text boxes

###### Chemical tests