Hellenic Accreditation System

Annex F1/13 to the Certificate No. 23-5

SCOPE of ACCREDITATION of the Laboratories of R&D and QUALITY DEPARTMENT of TITAN Cement Company S.A.

| Tested materials/ Products | Types of test/ Properties to be measured | Applied standards/Techniques to be used |
| --- | --- | --- |
| Physical Tests |
| Concrete | 1.Slump test of fresh concrete | Nat. Leg. ΣΚ-309 : 1986 ASTM C143/C 143M-15 :2015 |
|  | 2.Testing fresh concrete .Part 2: Slump test | ELOT ΕΝ 12350-2:2009 |
| Aggregates Aggregates(con.) | 1.Particle size distribution of aggregates | ΕLΟΤ ΕΝ 933-1: 2012 |
|  | 2.Determination of sand equivalent of soil and fine aggregate | ASTM D 2419:2014 |
|  | 3.Tests for geometrical properties of aggregates Part 8: Assesement of fines – Sand equivalent test | ELOT ΕΝ 933-8: 2012+A1:2015 |
|  | 4.Tests for geometrical properties of aggregates Part 9: Assessment of fines – Methylene Blue Test | ELOT ΕΝ 933-9:2009+A1:2013 |
|  | 5.Tests for geometrical properties of aggregates Part 4: Determination of particle shape – Shape index | ELOT ΕΝ 933-4: 2008 |
|  | 6.Tests for geometrical properties of aggregates Part 3: Determination of particle shape – Flakiness index | ELOT ΕΝ 933-3: 2012 |
| Mechanical tests |
| Concrete | 1.Preparation curing, and compressive strength determination of concrete cubic specimens | Nat. Leg. ΣK-304 : 1986 Nat. Leg. ΣK-303 : 1985 |
|  |  | ELOT ΕΝ 12390-2:2009 |
|  | 2.Testing hardened concrete - Part 3: Compressive strength of test specimens (cubic specimens up to 150.2mm dimensions) | ELOT ΕΝ 12390-3:2010 |
|  | 3.Vebe test | ELOT ΕΝ 12350.03:2009 |
| Chemical tests |
| Coal | Determination of total moisture | ISO 589:2008 Method A2 |
| Coke | Moisture determination | ISO 687:2010 |
| Coal/Coke | Determination of total sulfur | ISO 334:2013 |
| Solid mineral fuels | 1.Determination of ash content | ISO 1171:2010 |
|  | 2.Determination of total carbon, hydrogen and nitrogen | ISO 29541:2010 |
|  | 3.Determination of gross calorific value and calculation of net calorific value | ISO 1928:2009 |

| Tested materials/ Products | Types of test/ Properties to be measured | Applied standards/Techniques to be used |
| --- | --- | --- |
| Raw meal | 1.CO2 determination | In house method based on ELOT ΕΝ 196-2 :2013 §4 (Μ43) |
|  |  | In house method with the use of Differential Scanning calorimetry – Thermogravimetry (Μ45) |
|  | 2.Determination of major elements | In house method based on ELOT ΕΝ 196-2:2013 §4 (Μ44) |
|  | 3.Determination of total organic carbon (TOC) | In house method based on ELOT ΕΝ 13639:2017 §6 (Μ46) |
| Cement | 1.Determination of major elements | ELOT ΕΝ 196-2:2013 §4 |
|  | 2.Determination of the water –soluble chromium(VI) | ELOT ΕΝ 196-10:2016 |
| Limestone | Determination of total organic carbon (TOC) | ELOT ΕΝ 13639:2017 |

Site of assessment:     Permanent laboratory premises, Kamari Plant, Elefsis

Approved signatories: Ioannis Giannakopoulos, Emmanouil Tzanis

This Scope of Accreditation replaces the previous one dated 10.05.2019.

The Accreditation Certificate No. 23-4, to ELOT EN ISO/IEC 17025:2005, is valid until

04.07.2021.

Athens, 24.02.2020

Spyridon Podaras

Managing Director, ESYD