Hellenic Accreditation System

Annex F1/19 to the Certificate No. 364-7 SCOPE of ACCREDITATION of the Physicochemical Laboratory of the BUREAU VERITAS HELLAS S.M.S.A.

| Materials / Products tested | Types of test / Properties measured | Applied methods / Techniques used |
| --- | --- | --- |
| Physicochemical tests |
| Petroleum and petroleum products Petroleum and petroleum products (continued) Petroleum and petroleum products (continued) | 1. Determination of flash point (oC) | Pensky Martens closed cup method ISO 2719:2016 + A1-2021 ASTM D93:2020 IP34:2016 (Procedure Α and Β) (R2021) |
|  | 2. Determination of density (Kg/m3, g/cm3) | Hydrometer method ISO 3675:1998 ASTM D 1298:2012b (2017)e1 IP160:1999 |
|  | 3. Determination of distillation characteristics at atmospheric pressure | Distillation at atmospheric pressure ISO 3405:2019 ASTM D 86:2023 IP123:2011 (R2019) |
|  | 4. Determination of moisture (mg/Kg) | Coulometric Karl Fischer titration ISO 12937:2000 ASTM D 6304:2020 IP438:2001 (R2013) |
|  | 5. Determination of sulfur content (mg/kg) | Ultraviolet fluorescence method ISO 20846:2019 ASTM D 5453:2019a IP490:2019 (R2019) |
|  | 6. Determination of water content (% wt or % vol) | Distillation method ISO 3733:1999 ASTM D 95:2023 IP74:2000 (R2014) |
|  | 7. Determination of kinematic viscosity and calculation of dynamic viscosity (mm2/s, cSt) | Viscometer method ISO 3104:2023 ISO 3105:1994 ASTM D445:2021e2 ASTM D446:2012 (R2017) IP 71/1:1997 (R2020) IP 71/2:1995 (R 2004) |
|  | 8. Determination of pour point, (oC) | Pour point ISO 3016:2019 ASTM D 97:2017b (R2022) IP15:2017 |
|  | 9.Determination of sulfur content-energy dispersive X-ray fluorescence spectrometry | Sulfur content by XRF ISO 8754:2003 ASTM D 4294:2021 IP 336:2004 (R2022) |
|  | 10. Determination of carbon residue-micro method (MCR) | Micro carbon residue ISO 10370:2014 ASTM D 4530:2015 (R2020) IP 398:2015 (R2020) |
|  | 11. Determination of carbon, hydrogen, nitrogen | C, H, N determination by instrumental analysis ASTM D 5291:2021 |
|  | 12. Determination of ash | Ash determination ISO 6245:2001 ASTM D 482:2019 IP4:2005 (R2012) |
|  | 13. Determination of total sediment by hot filtration | IP 375:2011 (R2022) ISO 10307-1:2009 ASTM D 4870:2018 |
|  | 14. Determination of total sediment by thermal ageing (Procedure A) and chemical ageing (Procedure B) | ISO 10307-2:2009 (Cor 1:2010) IP 390:2011 (R.2017) ASTM D 4870:2018 |
|  | 15. Determination of aluminum and Silicon | ISO 10478:1994 (ICP technique) |
|  | 16. Determination of aluminum, silicon, sodium, vanadium, nickel, iron, calcium, zinc, phosphorous | IP 501:2005 (R2019) |
|  | 17. Heat of combustion of liquid hydrocarbon fuels by bomb calorimeter | ASTM D240:2019 |
|  | 18. Determination of density oscillating U-tube method | ASTM D 4052:2022 ISO 12185:1996, Cor1 2001 IP365:1997 (R2020) |
|  | 19.Standard test method for acid number of petroleum products by potentiometric titration | ASTM D 664:2018e2 |
|  | 20. Standard test method for dynamic viscosity and density of liquids by Stabinger viscometer (and calculation of kinematic viscosity) | ASTM D 7042:2021a |
|  | 21. Determination of fatty acid methyl ester (FAME) in middle distillates - IR method | IP 579:2014 EN 14078:2014 |
|  | 22. Determination of asphaltenes (heptane insoluble) in crude petroleum and petroleum products | IP 143:2004 (R2021) ASTM D 6560:2022 |
|  | 23. Base number of petroleum products by potentiometric perchloric acid titration | ASTM D2896:2021 ISO 3771:2011 method B (R2022) |
|  | 24. Standard Test Method for Sediment in Crude Oils and Fuel Oils by the Extraction Method, % wt | ISO 3735:1999 IP 53:2000(2014) ASTM D 473:2022 |
|  | 25. Standard Test Method for Flash and Fire Points by Cleveland Open Cup Tester, °C | ISO 2592:2017 IP 36:2002 ASTM D 92:2018 |
| Diesel and domestic heating fuels | 1. Determination of cold filter plugging point (oC) | Determination of cold filter plugging point (°C) ΕΝ 116:2015 IP 309:2016 ASTM D 6371:2017a |
| Petroleum | 1. Calculation of cetane index | CCI by four variable equation ASTM D 4737:2021 ISO 4264:2018 IP 380:2018 |
|  | 2. Cloud point (oC) | ISO 3015:2019 IP 219:2020 ASTM D 2500:2023 |
|  | 3. Assessment of lubricity using the high frequency reciprocating rig (HFRR) | ISO 12156-1:2023 ASTM D 6079:2022 IP450:2020 |
|  | 4. Determination of trace elements in middle distillate fuels by inductively coupled plasma atomic emission spectrometry (ICP-AES) | ASTM D 7111:2016 (R2021) |
|  | 5. Determination of oxidation stability of middle-distillate fuels, g/cm3 | ISO 12205:1995 IP388:1997 (R2022) ASTM D 2274:2014 (R2019) |

Site of asseseement:  Permanent laboratory premises, 12th km Athens-Lamia National Road, 14452, Metamorfosi, Attiki, Greece

Approved signatories: C.(S). Sotiriou, J. Gkolezakis, N. Kakali, M. Giannopoulos, S. Kontaki,      P. Kontos, P. Paterakis, T. Kitsonis, K. Tsiolis.

This Scope of Accreditation replaces the previous one dated 21.07.2023.

The Accreditation Certificate No. 364-7, to ELOT EN ISO/IEC 17025:2017, is valid until 9.07.2028.

Athens, 18.12.2023

Christos Nestoras

CEO of ESYD