Hellenic Accreditation System

Annex F1/20 to the Certificate No. 201-6 SCOPE of ACCREDITATION of the Laboratory of the Department of Materials and Quality Control of Sterea Ellada Public Works of the Directorate of Technical Inspection of the Directorate General for Spatial and Environmental Policy of the Decentralised administration Thessalias –Stereas Elladas

| Tested materials/ products | Types of test/ Properties to be measured | Applied Standards/ Techniques to be used |
| --- | --- | --- |
| Mechanical tests |
| Concrete | 3. Testing concrete in structures - Part 1: Cored specimens - Taking, examining and testing in compression | ELOT EN 12501-1:2020 Greek Concrete Regulation 2016 |
|  | 4.Testing hardened concrete - Part 3: Compressive strength of test specimens | ELOT ΕΝ 12390-3: 2019 Greek Concrete Regulation 2016 |
| Bituminous mixtures | 2.Bituminous mixtures - Test methods - Part 34: Marshall test | ΕLΟΤ ΕΝ 12697-34: 2020 |
|  | 3.Bituminous mixtures - Test methods - Part 30: Specimen preparation by impact compactor | ΕLΟΤ ΕΝ 12697-30: 2019 |
| Aggregates | 1.Tests for mechanical and physical properties of aggregates Part 2: Methods for the determination of resistance to fragmentation – Los Angeles test | ΕLΟΤ ΕΝ 1097-2: 2020 |
|  | 2.Tests for mechanical and physical properties of aggregates Part 1 : Determination of the resistance to wear (Micro –Deval) | ΕLΟΤ ΕΝ 1097-1: 2011 |
| Physical tests |
| Concrete | 2.Bituminous mixtures - Test methods - Part 2: Determination of particle size distribution | ΕLΟΤ EN 12697-2:2015 + A1 :2019 |
| Aggregates | 1.Sieve analysis of fine and coarse aggregates | National Specification Ε105-86, Test 7 |
|  | 2.Determination of the sand equivalent | ASTM D 2419-22 |
|  | 3.Tests for geometrical properties of aggregates Part 1: Determination of particle distribution – Sieving method | ELOT ΕΝ 933-1: 2012 +A1:2015 |
| Aggregates | 1.Sieve analysis of fine and coarse aggregates | National Specification Ε105-86, Test 7 |
|  | 2.Determination of the sand equivalent | ASTM D 2419-22 |
|  | 3.Tests for geometrical properties of aggregates Part 1: Determination of particle distribution – Sieving method | ELOT ΕΝ 933-1: 2012 +A1:2015 |
|  | 4.Tests for geometrical properties of aggregates Part 8: Assessment of fines – Sand equivalent test | ELOT ΕΝ 933-8: 2012 |
|  | 5.Tests for geometrical properties of aggregates Part 3: Determination of particle shape – Flakiness Index | ELOT ΕΝ 933-3: 2012 |
| Aggregates & Soils | Determination of the amount of material finer than No 200 (0,075 mm) sieve | National Specification Ε105-86, Test 8 |
| Soils | 1.Soil compaction test (modified Proctor method) | National Specification Ε105-86 (4 alternative methods A,B,C,D) Test 11 |
|  | 2.Determination of the liquid limit, the plastic limit and the plasticity index of soils | National Specification Ε105-86, Tests 5 & 6 |
|  | 3.Determination of the moisture of soils | National Specification Ε105-86, Test 2 |
| Chemical tests |
| Bituminous mixtures | 2.Bituminous mixtures - Test methods for hot mix asphalt - Part 1: Soluble binder content | ELOT EN 12697-1:2020, ANNEX B §. Β.1.5. & Β.2 |

Site of assessment: Laboratory permanent premises, 17 Elikonos Str., Lamia, Greece

Approved signatories: Ch. Tsimpouris

This Scope of Accreditation replaces the previous one dated 01.11.2022.

The Accreditation Certificate No. 201-6, to ELOT EN ISO/IEC 17025:2017, is valid until 17.05.2025.

Athens, 25.09.2023

Christos Nestoras

CEO of ESYD