Hellenic Accreditation System

Annex F1/12 to the Certificate No. 428-7 SCOPE of ACCREDITATION of the Quality Control Laboratory of MYTILINEOS S.A. METALLURGY BUSINESS UNIT Plant Aluminium of Greece, Agios Nicolaos, Viotia

| Materials / Products to be tested | Types of test / Properties to be measured | Applied methods / Techniques to be used |
| --- | --- | --- |
|  | Physical tests |
| Aluminium Ores | % Humidity | Aluminium ores: Determination of humidity In house (M-ΒΩ-0002) |
| Hydrate Alumina | % Passing from the sieve 45μm (% -45μm) | Aluminium oxide used for the production of primary aluminium – Particle size analysis for the range 45μm to 150μm – method using electroformed sieves ISO 2926:2013 |
|  | % Passing from the sieve 75μm (% -75μm) |  |
| Calcined Alumina | % Retaining on the sieve 150μm (% +150μm) | Aluminium oxide used for the production of primary aluminium – Particle size analysis for the range 45μm to 150μm – method using electroformed sieves ISO 2926:2013 |
|  | % Passing from the sieve 75μm (% -75μm) |  |
|  | % Passing from the sieve 45μm (% -45μm) |  |
|  | Specific area m2/gr | Aluminium oxide used for the production of primary aluminium – determination of specific surface area by nitrogen absorption ISO 8008:2005 (E) |
|  | Attrition index | Alumina - Determination of attrition index ISO 17500:2006 |
| Chemical tests |
| Aluminium Ores | % Al2O3 | Aluminium ores: Chemical analysis- X-ray fluorescence spectrometric method In house (M-ΒΩ-0010) |
|  | % Fe2O3 |  |
|  | % SiO2 |  |
|  | % CaO |  |
|  | % S |  |
|  | % TiO2 |  |
|  | % V2O5 |  |
|  | % Zn |  |
|  | % LOI 105-1000oC | Aluminium ores: Determination of loss of mass at 1000oC AS 2932.3-2004 |
| Hydrate and Calcined Alumina | CaΟ ppm | Alumina: Determination of trace elements – Wavelength dispersive X-ray fluorescence spectrometric method AS 2879.7-1997 |
|  | Fe2Ο3 ppm |  |
|  | Ga2Ο3 ppm |  |
|  | Na2O ppm |  |
|  | P 2O5 ppm |  |
|  | S ppm |  |
|  | SiO2 ppm |  |
|  | TiO2 ppm |  |
|  | V2O5 ppm |  |
|  | ZnO ppm |  |
| Calcined Alumina | % a-Al2O3 | Alumina – Determination of alpha alumina content by X-ray diffraction- In house (M-ΑΔ-0008) |
|  | % Hydrargillite | Alumina – Determination of Hydrargillite content by X-ray diffraction- In house (M-ΑΔ-0037) |
|  | % LOI (300-1000oC) | Alumina – Determination of loss of mass at 300 and 1000oC ISO 806:2004 |
|  | Li2O ppm | Alumina – Determination of lithium – Atomic absorption spectroscopy In house (M-ΑΔ-0005) |
| Lime | % CO2 | Lime: Determination of % CO2 TGA701 In house (M-ΑΔ/ΒΩ-0004) |
| Aluminium and Aluminium Alloys | % As | Standard Practice for Analysis of Aluminium and Aluminium Alloys by Atomic Emission Spectrometry ASTM E 1251-17a |
|  | %B |  |
|  | % Ca |  |
|  | % Cd |  |
|  | % Cr |  |
|  | % Cu |  |
|  | % Fe |  |
|  | % Ga |  |
|  | % Li |  |
|  | % Mg |  |
|  | % Mn |  |
|  | % Na |  |
|  | % Ni |  |
|  | % Pb |  |
|  | % Si |  |
|  | % Ti |  |
|  | % V |  |
|  | % Zn |  |
|  | % Zr |  |
|  | % Βi |  |
|  | % Be |  |
|  | % Co |  |
|  | % Hg |  |

Site of assessment: Permanent laboratory premises, Plant Aluminium of Greece, Agios Nikolaos, Viotia, Greece.

Approved signatories: Vasiliki Vasiliadou, Paraskevi Soupsana, Athina Filippou, Sotirios Dimou.

This Scope of Accreditation replaces the previous one dated 21.04.2021.

The Accreditation Certificate No. 428-7, to ELOT EN ISO/IEC 17025: 2017, is valid until 25.05.2024.

Athens, 3.05.2022

Christos Nestoras

CEO of ESYD