Hellenic Accreditation System

Annex F1/15 to the Certificate No. 258-6 SCOPE of ACCREDITATION of the Testing Laboratory GEORGIOS DIDASKALOU & CO. Ltd.(GEOTER- DIDASKALOU L.P.)

| Tested materials / Products | Types of test / Properties to be measured / Procedures | Standards / Techniques to be used |
| --- | --- | --- |
| Physical tests |
| Hardened Concrete | Curing concrete cube test specimens (15cm x 15cm x 15cm) for compressive strength test | ΕLOT ΕΝ 12390.02-19 § 5.5 ΣΚ –303, § 5 |
| Aggregates | Tests for geometrical properties of aggregates – Part 1: Determination of particle size distribution – Sieving method | ΕLOT ΕΝ 933.01-12 & ΕLOT ΕΝ 932.02-00 |
|  | Tests for geometrical properties of aggregates – Part 3: Determination of particle shape-Flakiness index | ΕLOT ΕΝ 933.03-12 ΕLOT ΕΝ 932.02-00 |
|  | Tests for geometrical properties of aggregates – Part 4: Determination of particle shape, Shape index | ΕLOT ΕΝ 933.04-08 ΕLOT ΕΝ 932.02-00 |
|  | Tests for geometrical properties of aggregates – Part 8: Assessment of fines – Sand equivalent test | ΕLOT ΕΝ 933.08- 15 ΕLOT ΕΝ 932.02-00 |
|  | Test for mechanical and physical properties of aggregates - Part 6: Determination of particle density and water absorption | ΕLOT ΕΝ 1097.06-13 ΕLOT ΕΝ 932.02-00 |
|  | Tests for thermal and weathering properties of aggregates- Part 2: Magnesium sulfate test | ΕLOT ΕΝ 1367.02-10 & ΕLOT ΕΝ 13450-03 (Annex C) ΕLOT ΕΝ 932.02-00 |
| Mechanical tests |
| Aggregates | Test for mechanical and physical properties of aggregates - Part 1: Determination of the resistance to wear (micro-Deval) | ΕLOT EN 1097.01-11 |
|  | Test for mechanical and physical properties of aggregates – Part 2: Μethods for the determination of resistance to fragmentation, Test Los Angeles | ΕLOT ΕΝ 1097.02-20 |
|  | Test for mechanical and physical properties of aggregates – Part 3: Determination of loose bulk density and voids | ΕLOT ΕΝ 1097.03-99 |
| Hardened Concrete | Determination of compressive strength of concrete cube test specimens (15cm x 15cm x 15cm) & concrete cores | ΕLOT ΕΝ 12390.03-19, SΚ –304 (ΚΤΣ-2016) |
|  | Sampling of concrete cores | Ε-7, ΚΤS-97§ 13.7 (ΚΤΣ-2016), ΕΝ 12504.01-19 |
|  | Capping of concrete cores | ASTM C 617/C617M-15 |
| Chemical tests |
| Aggregates | Tests for geometrical properties of aggregates - Part 9: Assessment of fines – Methylene blue test | ΕLOT ΕΝ 933.09-13 |

Site of assessment: Permanent Premises, 20 Tombazi Street, P.O. box 21028, PostCode 55510, Greece

Approved signatories: Vassilios Didaskalou, Grigorios Didaskalou

This Scope of Accreditation replaces the previous one dated February 16th, 2022.

The Accreditation Certificate No 258-6, to ELOT EN ISO/IEC 17025:2005, is valid until February 20th, 2026.

Athens, 18.02.2022

Christos Nestoras

CEO of ESYD